LUMINESCENCE ANALYSIS OF CERAMICS FROM SOUTH KOREA

11 June 2015

James K. Feathers

Luminescence Dating Laboratory

University of Washington

Seattle, WA 98195-3412

Email: jimf@u.washington.edu

This report presents the results of luminescence analysis of eight ceramic samples collected from house pits at prehistoric sites in South Korea.  The samples were submitted by Seungki Kwak, PhD student at the University of Washington.   Table 1 lists the samples, provenance information, and expected age.  Laboratory procedures are given in the appendix.

Table 1.  Samples

| UW Lab # | City | Site | Provenance | House Pit # | Expected Age (basis) |
| --- | --- | --- | --- | --- | --- |
| UW3039 | Hoengseong | Eupha-Ri | 5-1 | 1 | 1850-1650 BP (C-14) |
| UW3040 | Hoengseong | Eupha-Ri | 5-1 | 2 | 1850-1650 BP (C-14) |
| UW3041 | Hoengseong | Eupha-Ri | 5 | 14 | 1850-1650 BP (C-14) |
| UW3042 | Pyeong-taek | Sosa-Dong | Ra | 4 | 3400-3000 BP (ceramics) |
| UW3043 | Pyeong-taek | Sosa-Dong | Ra | 14 | 3400-3000 BP (ceramics) |
| UW3044 | Pyeong-taek | Sosa-Dong | Ra | 43 | 3400-3000 BP (ceramics) |
| UW3045 | Kimpo | Kimpo-Yanchon | 2-1 (L) | 3 | 3090-2540 BP (C-14) |
| UW3046 | Kimpo | Kimpo-Yanchon | 2-1 (D) | 10 | 3090-2540 BP (C-14) |

Dose rate

The dose rate was measured on each ceramic but an associated sediment was not available for any sample.   Average sediment dose rates drawn from four publications of luminescence dating in South Korea were used as an estimate, with the standard deviation as the error (Kim et al. 2010, Hong et al. 2001, 2003, Lim et al. 2007).  Because the gamma dose rate contributes on average only about 20% of the total dose rate, the uncertainty from using published data is tolerable.   Relevant dose rate concentrations are given in Table 2.

Dose rates on the ceramics were mainly determined using alpha counting and flame photometry.  The beta dose rate calculated from these measurements on the ceramics was compared with the beta dose rate measured directly by beta counting.   Table 2 compares the beta dose rate calculated in the two ways mentioned.  These did not differ at one-sigma for any sample.  Moisture content was estimated as 80 ± 20 % of saturated value for the ceramic sherds, and 22 ± 6 percent for the sediments, reflecting loamy sediments in a temperate environment.  Burial depth was not known precisely but was estimated at 25-30 cm for all samples.   Table 3 gives total dose rates for each sample.  Dose rates ranged from 4.0 to 5.6 Gy/ka.

Table 2.  Radionuclide concentrations

| Sample | 238U (ppm) | 233Th (ppm) | K (%) | Beta dose rate (Gy/ka) |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | ß-counting | α-counting/flame photometry |
| UW3039 | 1.44±0.25 | 22.71±2.10 | 2.45±0.06 | 2.88±0.24 | 2.85±0.08 |
| UW3040 | 2.60±0.18 | 5.75±0.99 | 2.31±0.20 | 2.67±0.24 | 2.43±0.17 |
| UW3041 | 2.11±0.28 | 22.67±2.18 | 2.82±0.06 | 3.35±0.28 | 3.28±0.09 |
| UW3042 | 2.12±0.30 | 26.96±2.36 | 2.40±0.06 | 3.03±0.26 | 3.03±0.09 |
| UW3043 | 2.01±0.31 | 30.20±2.35 | 2.24±0.24 | 2.72±0.24 | 2.96±0.21 |
| UW3044 | 3.17±0.26 | 15.81±1.59 | 2.03±0.06 | 2.48±0.20 | 2.56±0.08 |
| UW3045 | 2.20±0.21 | 12.52±1.49 | 1.81±0.04 | 2.40±0.20 | 2.15±0.06 |
| UW3046 | 2.04±0.19 | 10.43±1.34 | 2.27±0.05 | 2.65±0.23 | 2.45±0.06 |
| sediment | 3.43±0.50 | 9.15±3.00 | 2.14±0.50 |  |  |

Table 3.  Dose rates (Gy/ka)*

| Sample | alpha | beta | gamma | cosmic | total |
| --- | --- | --- | --- | --- | --- |
| UW3039 | 0.56±0.04 | 2.50±0.11 | 1.17±0.16 | 0.18±0.04 | 4.41±0.20 |
| UW3040 | 0.59±0.04 | 2.14±0.16 | 1.09±0.16 | 0.18±0.04 | 4.00±0.23 |
| UW3041 | 1.35±0.10 | 2.91±0.11 | 1.20±0.16 | 0.18±0.04 | 5.64±0.22 |
| UW3042 | 1.18±0.14 | 2.56±0.13 | 1.18±0.16 | 0.18±0.04 | 5.09±0.25 |
| UW3043 | 0.89±0.06 | 2.48±0.20 | 1.19±0.16 | 0.18±0.04 | 4.74±0.27 |
| UW3044 |  |  |  |  |  |
| UW3045 | 1.50±0.10 | 1.86±0.08 | 1.11±0.16 | 0.18±0.04 | 4.65±0.21 |
| UW3046 | 0.86±0.09 | 2.13±0.09 | 1.10±0.16 | 0.18±0.04 | 4.27±0.20 |

* Dose rates for ceramics are calculated for OSL.  They will usually be higher for TL and IRSL due to higher b-values.   Also the beta dose rate is lower than that given in Table 2 due to moisture correction.

Equivalent Dose

Equivalent dose was measured for TL, OSL and IRSL as described in the appendix.   TL plateaus (Table 4), ranged from 60 to 180°C in breadth, with only two samples having plateau breadths less than 100°C.   All but UW3039 and UW3042 showed a sensitivity change with heating.  TL anomalous fading was evident in all samples. Anomalous fading rates, or g-values, ranged from 7 to 15%, with a median of 9.  Only on UW3041 was the fading rate so high that the correction produced an infinite age, indicating the fading rate was either over-estimated or changed through time.   Correction for fading followed Huntley and Lamothe (2001).

Table 4.  TL parameters

| Sample | Plateau (°C) | 1st/2nd ratio* | fit | Fading g-value** |
| --- | --- | --- | --- | --- |
| UW3039 | 250-310 | 1 | linear | 8.1±2.2 |
| UW3040 | 250-370 | 2.24±0.55 | linear | 6.8±3.6 |
| UW3041 | 280-390 | 2.00±0.12 | linear | 15.9±5.5 |
| UW3042 | 290-370 | 1 | linear | 13.1±4.9 |
| UW3043 | 250-420 | 2.60±0.26 | linear | 9.2±5.3 |
| UW3044 |  |  |  |  |
| UW3045 | 250-430 | 1.73±0.36 | quadratic | 7.7±2.4 |
| UW3046 | 250-420 | 1.93±0.32 | linear | 10.1±4.4 |

*Refers to slope ratio between the first and second glow growth curves.  A glow refers to luminescence as a function of temperature; a second glow comes after heating to 450°C.

** A g-value is a rate of anomalous fading, measured as percent of signal loss per decade, where a decade is a power of 10.

OSL/IRSL was measured on 6 aliquots per sample (Table 5).  Scatter was low (less than 10% over-dispersion) on all samples.   An IRSL signal could be measured on all samples but it was weaker than the OSL signal by 2 to 20 times.  Ceramics were heated when made and that has a tendency to increase the quartz signal and reduce the feldspar signal.   IRSL stems from feldspars, which are prone to anomalous fading.  A relatively large IRSL signal may suggest the OSL signal partly stems from feldspars and therefore may fade, while a weak IRSL suggests the OSL is dominated by quartz.  Another measure of feldspar contribution is the size of the OSL b-value.  The b-value is a measure of alpha luminescence efficiency, and is usually less than 0.7 for quartz and higher than that for feldspar.  For these samples the average was 0.98, with all but two samples having values greater than 0.7.  This suggests feldspars are making some contribution to the OSL signal.   Fading was only measured on the TL signal, because of exorbitant machine time required to measure fading for OSL and IRSL.  As a test of the SAR procedures, a dose recovery test was performed.  The recovered dose was within two-sigma of the given dose for all but UW3045. Equivalent dose and b-values are given in Table 6.

Table 5.  OSL/IRSL data

| Sample | # aliquots* |  | OSL Over-dispersion (%) | Dose Recovery (OSL) |  |
| --- | --- | --- | --- | --- | --- |
|  | OSL | IRSL |  | Given Dose (sß) | Recovered Dose (sß) |
| UW3039 | 5 | 6 | 0** | 100 | 96.8±6.3 |
| UW3040 | 6 | 6 | 0 | 60 | 62.2±3.5 |
| UW3041 | 5 | 6 | 0** | 80 | 79.6±4.2 |
| UW3042 | 6 | 6 | 6.2±2.4 | 100 | 92.3±4.2 |
| UW3043 | 6 | 6 | 0 | 100 | 99.0±6.6 |
| UW3044 |  |  |  |  |  |
| UW3045 | 6 | 6 | 3.9±2.3 | 60 | 52.3±2.2 |
| UW3046 | 6 | 6 | 6.7±2.8 | 80 | 81.2±3.8 |

* Denotes number of aliquots with measurable signals.

** Over-dispersion after outliers removed.

Table 6. Equivalent dose and b-value – fine grains

| Sample | Equivalent Dose (Gy) |  |  | b-value (Gy µm2) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | TL | IRSL | OSL | TL | IRSL | OSL* |
| UW3039 | 14.7±1.07 | 14.7±2.54 | 8.16±0.264 | 2.19±0.294 | 0.905±0.046 | 0.483±0.022 |
| UW3040 | 10.9±3.22 | 10.0±0.214 | 8.97±0.160 | 3.01±1.06 | 1.45±0.042 | 0.934±0.025 |
| UW3041 | 7.92±0.598 | 8.53±0.326 | 8.58±0.186 | 1.74±0.114 | 1.23±0.053 | 1.03±0.054 |
| UW3042 | 18.9±1.11 | 13.2±0.307 | 14.5±0.430 | 2.83±0.217 | 1.29±0.047 | 0.860±0.083 |
| UW3043 | 14.0±1.47 | 14.2±0.591 | 12.0±0.229 | 1.91±0.153 | 1.38±0.062 | 0.608±0.021 |
| UW3044 |  |  |  |  |  |  |
| UW3045 | 13.6±3.55 | 11.1±0.429 | 12.8±0.296 | 2.28±0.474 | 1.83±0.063 | 1.80±0.060 |
| UW3046 | 10.8±2.03 | 10.2±0.445 | 11.8±0.389 | 2.42±0.401 | 1.43±0.040 | 1.18±0.096 |

Ages

Table 7 gives the derived ages for each sample.  They will be discussed by site:

1)  Eupha-Ri  - - The OSL signal for UW3039 is most likely from quartz.  The IRSL signal is weak and the OSL b-value is well in the range of quartz.  The uncorrected (for fading) TL age is older but only by about 120 years.  A 15-day storage after irradiation probably minimized fading.  The OSL age is the best estimate.  The ages for OSL, IRSL and uncorrected TL are all in agreement for UW3040.  Any fading is not significant.  The ages for OSL and IRSL are in agreement for UW3041, and should be the best estimate.  The TL age is younger probably because of fading issues unresolved because of a very high measured fading rate.   The ages range from BC 260 to AD 530, somewhat broader than the range of 14C ages

2) Sosa-Dong – The OSL and uncorrected TL ages are in agreement for UW3042, and TL fading is insignificant.  The IRSL age is younger, probably because of fading.  The OSL, IRSL and uncorrected TL ages are in agreement for UW3043.  Fading is not significant.  UW3044 is not completed.   The two ages calculated so far are younger by a few hundred years than the 14C range.

3) Kimpo-Yanchon – The OSL and uncorrected TL ages are in agreement for UW3045, and TL fading is not significant.  The IRSL age is younger, probably due to fading.  The OSL age is the best estimate for UW3046.  The corrected TL age is not significantly different from the OSL age but with high error.  The IRSL age is younger, probably due to fading.  The two ages are on the young side of the 14C range.

For all samples but UW3039, the fading correction does not result in an age estimate that is significantly different from the uncorrected age.  This is partly due to high error terms, but the uncorrected age also agrees with the OSL ages in most cases.   This might suggest that the fading corrections are not very accurate.  The OSL b-value is over 1 for UW3041, UW3045, and UW3046, suggesting the OSL signal may also fade some for these samples.  The ages for these three could be slight underestimations.

Table 7.  Ages

| Sample | Age (ka) | % error | Basis for age | Calendar date |
| --- | --- | --- | --- | --- |
| UW3039 | 1.85±0.12 | 6.3 | OSL | AD 160 ± 120 |
| UW3040 | 2.28±0.11 | 4.7 | OSL/IRSL/uncorrected TL | BC 260 ± 110 |
| UW3041 | 1.49±0.06 | 4.1 | OSL/IRSL | AD 530 ± 60 |
| UW3042 | 2.66±0.14 | 5.2 | OSL/uncorrected TL | BC 650 ± 140 |
| UW3043 | 2.41±0.11 | 4.6 | OSL/IRSL/uncorrected TL | BC 390 ± 110 |
| UW3044 |  |  |  |  |
| UW3045 | 2.75±0.16 | 5.8 | OSL/ uncorrected TL | BC 740 ± 160 |
| UW3046 | 2.76±0.18 | 6.6 | OSL | BC 740 ± 180 |

Appendix:

Procedures for Thermoluminescence Analysis of Pottery

Sample preparation -- fine grain

The sherd is broken to expose a fresh profile.  Material is drilled from the center of the cross-section, more than 2 mm from either surface, using a tungsten carbide drill tip.  The material retrieved is ground gently by an agate mortar and pestle, treated with HCl, and then settled in acetone for 2 and 20 minutes to separate the 1-8 µm fraction.  This is settled onto a maximum of 72 stainless steel discs.

Glow-outs

Thermoluminescence is measured by a Daybreak reader using a 9635Q photomultiplier with a Corning 7-59 blue filter, in N2 atmosphere at 1°C/s to 450°C.  A preheat of 240°C with no hold time precedes each measurement.  Artificial irradiation is given with a 241Am alpha source and a 90Sr beta source, the latter calibrated against a 137Cs gamma source.  Discs are stored at room temperature for at least one week after irradiation before glow out.  Data are processed by Daybreak TLApplic software.

Fading test

Several discs are used to test for anomalous fading.  The natural luminescence is first measured by heating to 450°C.  The discs are then given an equal alpha irradiation and stored at room temperature for varied times: 10 min, 2 hours, 1 day, 1 week and 8 weeks.  The irradiations are staggered in time so that all of the second glows are performed on the same day.  The second glows are normalized by the natural signal and then compared to determine any loss of signal with time (on a log scale).  If the sample shows fading and the signal versus time values can be reasonably fit to a logarithmic function, an attempt is made to correct the age following procedures recommended by Huntley and Lamothe (2001).  The fading rate is calculated as the g-value, which is given in percent per decade, where decade represents a power of 10.

Equivalent dose

The equivalent dose is determined by a combination additive dose and regeneration (Aitken 1985).  Additive dose involves administering incremental doses to natural material.  A growth curve plotting dose against luminescence can be extrapolated to the dose axis to estimate an equivalent dose, but for pottery this estimate is usually inaccurate because of errors in extrapolation due to nonlinearity.  Regeneration involves zeroing natural material by heating to 450°C and then rebuilding a growth curve with incremental doses.  The problem here is sensitivity change caused by the heating.  By constructing both curves, the regeneration curve can be used to define the extrapolated area and can be corrected for sensitivity change by comparing it with the additive dose curve.  This works where the shapes of the curves differ only in scale (i.e., the sensitivity change is independent of dose).  The curves are combined using the “Australian slide” method in a program developed by David Huntley of Simon Fraser University (Prescott et al. 1993).  The equivalent dose is taken as the horizontal distance between the two curves after a scale adjustment for sensitivity change.  Where the growth curves are not linear, they are fit to quadratic functions.  Dose increments (usually five) are determined so that the maximum additive dose results in a signal about three times that of the natural and the maximum regeneration dose about five times the natural.

A plateau region is determined by calculating the equivalent dose at temperature increments between 240° and 450°C and determining over which temperature range the values do not differ significantly.  This plateau region is compared with a similar one constructed for the b-value (alpha efficiency), and the overlap defines the integrated range for final analysis.

Alpha effectiveness

Alpha efficiency is determined by comparing additive dose curves using alpha and beta irradiations.  The slide program is also used in this regard, taking the scale factor (which is the ratio of the two slopes) as the b-value (Aitken 1985).

Radioactivity

Radioactivity is measured by alpha counting in conjunction with atomic emission for 40K.  Samples for alpha counting are crushed in a mill to flour consistency, packed into plexiglass containers with ZnS:Ag screens, and sealed for one month before counting.  The pairs technique is used to separate the U and Th decay series. For atomic emission measurements, samples are dissolved in HF and other acids and analyzed by a Jenway flame photometer.  K concentrations for each sample are determined by bracketing between standards of known concentration.  Conversion to 40K is by natural atomic abundance.  Radioactivity is also measured, as a check, by beta counting, using a Risø low level beta GM multicounter system.   About 0.5 g of crushed sample is placed on each of four plastic sample holders.  All are counted for 24 hours.  The average is converted to dose rate following Bøtter-Jensen and Mejdahl (1988) and compared with the beta dose rate calculated from the alpha counting and flame photometer results.

Both the sherd and an associated soil sample are measured for radioactivity.  Additional soil samples are analyzed where the environment is complex, and gamma contributions determined by gradients (after Aitken 1985: appendix H).  Cosmic radiation is determined after Prescott and Hutton (1994).   Radioactivity concentrations are translated into dose rates following Guérin et al. (2011).

Moisture Contents

Water absorption values for the sherds are determined by comparing the saturated and dried weights.  For temperate climates, moisture in the pottery is taken to be 80 ± 20 percent of total absorption, unless otherwise indicated by the archaeologist.  Again for temperate climates, soil moisture contents are taken from typical moisture retention quantities for different textured soils (Brady 1974: 196), unless otherwise measured.  For drier climates, moisture values are determined in consultation with the archaeologist.

Procedures for Optically Stimulated or Infrared Stimulated Luminescence of Fine-grained pottery.

Optically stimulated luminescence (OSL) and infrared stimulated luminescence (IRSL) on fine-grain (1-8µm) pottery samples are carried out on single aliquots following procedures adapted from Banerjee et al. (2001) and Roberts and Wintle (2001.  Equivalent dose is determined by the single-aliquot regenerative dose (SAR) method (Murray and Wintle 2000).

The SAR method measures the natural signal and the signal from a series of regeneration doses on a single aliquot.  The method uses a small test dose to monitor and correct for sensitivity changes brought about by preheating, irradiation or light stimulation.  SAR consists of the following steps: 1) preheat, 2) measurement of natural signal (OSL or IRSL), L(1), 3) test dose, 4) cut heat, 5) measurement of test dose signal, T(1), 6) regeneration dose, 7) preheat, 8) measurement of signal from regeneration, L(2), 9) test dose, 10) cut heat, 11) measurement of test dose signal, T(2), 12) repeat of steps 6 through 11 for various regeneration doses.  A growth curve is constructed from the L(i)/T(i) ratios and the equivalent dose is found by interpolation of L(1)/T(1).  Usually a zero regeneration dose and a repeated regeneration dose are employed to insure the procedure is working properly.  For fine-grained ceramics, a preheat of 240°C for 10s, a test dose of 3.1 Gy, and a cut heat of 200°C are currently being used, although these parameters may be modified from sample to sample.

The luminescence, L(i) and T(i), is measured  on a Risø TL-DA-15 automated reader by a succession of two stimulations: first 100 s at 60°C of IRSL (880nm diodes), and then 100s at 125°C of OSL (470nm diodes).  Detection is through 7.5mm of Hoya U340 (ultra-violet) filters.  The two stimulations are used to construct IRSL and OSL growth curves, so that two estimations of equivalent dose are available.  Anomalous fading usually involves feldspars and only feldspars are sensitive to IRSL stimulation.  The rationale for the IRSL stimulation is to remove most of the feldspar signal, so that the subsequent OSL (post IR blue) signal is free from anomalous fading.  However, feldspar is also sensitive to blue light (470nm), and it is possible that IRSL does not remove all the feldspar signal.  Some preliminary tests in our laboratory have suggested that the OSL signal does not suffer from fading, but this may be sample specific.  The procedure is still undergoing study.

A dose recovery test is performed by first zeroing the sample by exposure to light and then administering a known dose.  The SAR protocol is then applied to see if the known dose can be obtained.

Alpha efficiency will surely differ among IRSL, OSL and TL on fine-grained materials.  It does differ between coarse-grained feldspar and quartz (Aitken 1985).  Research is currently underway in the laboratory to determine how much b-value varies according to stimulation method.  Results from several samples from different geographic locations show that OSL b-value is less variable and centers around 0.5.  IRSL b-value is more variable and is higher than that for OSL.  TL b-value tends to fall between the OSL and IRSL values.  We currently are measuring the b-value for IRSL and OSL by giving an alpha dose to aliquots whose luminescence have been drained by exposure to light.  An equivalent dose is determined by SAR using beta irradiation, and the beta/alpha equivalent dose ratio is taken as the b-value.  A high OSL b-value is indicative that feldspars might be contributing to the signal and thus subject to anomalous fading.

.

Age and error terms

The age and error for both OSL and TL are calculated by a laboratory constructed spreadsheet, based on Aitken (1985).  All error terms are reported at 1-sigma.

References

Adamiec, G., and Aitken, M. J., 1998, Dose rate conversion factors: update.  Ancient TL 16:37-50.

Aitken,  M. J., 1985, Thermoluminescence Dating, Academic Press, London.

Banerjee, D., Murray, A. S., Bøtter-Jensen, L., and Lang, A., 2001, Equivalent dose estimation using a single aliquot of polymineral fine grains.  Radiation Measurements 33:73-93.

Bøtter-Jensen, L, and Mejdahl, V., 1988, Assessment of beta dose-rate using a GM multi-counter system.  Nuclear Tracks and Radiation Measurements 14:187-191.

Brady, N. C., 1974,  The Nature and Properties of Soils, Macmillan, New York.

Guérin, G., Mercier, N., and Adamiec, G., 2011, Dose-rate converstion factors: update.  Ancient TL 29:5-8.

Huntley, D. J., and Lamothe, M., 2001, Ubiquity of anomalous fading in K-feldspars, and measurement and correction for it in optical dating.  Canadian Journal of Earth Sciences 38:1093-1106.

Mejdahl, V., 1983, Feldspar inclusion dating of ceramics and burnt stones.  PACT 9:351-364.

Murray, A. S., and Wintle, A. G., 2000, Luminescence dating of quartz using an improved single-aliquot regenerative-dose protocol.  Radiation Measurements 32:57-73.

Prescott, J. R., Huntley, D. J., and Hutton, J. T., 1993, Estimation of equivalent dose in thermoluminescence dating – the Australian slide method.  Ancient TL 11:1-5.

Prescott, J. R., and Hutton, J. T., 1994, Cosmic ray contributions to dose rates for luminescence and ESR dating: large depths and long time durations.  Radiation Measurements 23:497-500.

Roberts, H. M., and Wintle, A. G., 2001, Equivalent dose determinations for polymineralic fine-grains using the SAR protocol: application to a Holocene sequence of the Chinese Loess Plateau.  Quaternary Science Reviews 20:859-863.

For a general review of luminescence dating by the director of this laboratory, see:

Feathers, J. K, 2003, Use of luminescence dating in archaeology.  Measurement Science and Technology 14:1493-1509

.